Appendix

1Ambiant and heating tests

20D45SWS test: sws connection with a 45 mm timber member and two steel plates on each side (12mm).

20DSWS6: sws connection, 63 mm timber member, one bolt, and two steel plates on each side (12mm)

20DSWS7: sws connection, 63 mm thickness, 12mm steel plates on the sides.

20DSWS8: sws connection, 63 mm thickness, 12 mm steel plates on the sides.

20SWS452: sws connection, one bolt, 45 mm timber, 12 mm steel plates on the sides.

20SWS453: sws connection, one bolt, 45 mm timber, 12 mm steel plates.

100sws45: 100 C heating test, sws connection, 45 mm timber, 6 mm steel plates.

150sswsb: 150 C heating test, sws connection,

200ssws5: 200 C heating test, sws connection, 63 mm timber, 6 mm steel plates.

200ssws45: 200 C heating test, sws connection, 45 mm timber, 6 mm steel plate.

280ssws3: 280 C heating test, sws connection, 63 mm timber, 6 mm steel plates.

280ssws4

2 Fire test

750ssws4: sws connection with one bolt

750ssws5: fire test, sws connection, one bolt.

750ssws6: fire test, sws connection, one bolt.

750msws1: fire test, sws connection, 4 bolts.

750msws2: fire test, sws connection, 4 bolts.

750msws3: sws connection, 4 bolts

750swsw: wsw connection, one bolt

750swsw2: wsw connection, one bolt.

750mwsw: invalided results (problems with the furnace)

750mwsw2: wsw connection with 4 bolts.

750mwsw3: wsw connection with 4 bolts.

750swww: www connection with one bolt.

750swww2: www connection with one bolt.

750mwww: www connection with 5 bolts

750mwww2

3 Pictures of some connections:

www connection with 5 bolts after a fire test

Sws connection with one bolt after a fire test

Wsw connection with one bolt after a fire test

4 Pictures of modes of failure:

Sws connection with for bolts after a fire test once the char has been removed. The mode of failure is mode j (the timber is crushed)

www connection with 5 bolts after a fire test.

The timber on the side members is crushed so this is mode g.

100 C heating test on a sws connection made of 45 mm timber.

The bolt are straight so the mode of failure is mode j.

Ambient test on a sws connection with 63 mm timber and 12 mm steel plates on the sides. The bolts seems to be bent on mode m.

Ambient test on a sws connection with 45 mm timber and 12 mm steel plates on the sides. The bolts are straight so the failure is mode.

280 C heating test on a sws connection with 63 mm timber. The wood started charring on the sides. The bolts are straight so this is mode j.

5 Prediction of time to failure using Johansen’s equation with the results from the tests:

6 Safir results

Sws connection:

Wsw connection:

www connection

7 Manufacturing process of LVL timber

# Text boxes

Diagram Load-displacement for a sws connection at 20 degree C (20D45sws)

0

5

10

15

20

25

0

2

4

6

8

10

12

14

16

18

20

Deformation (mm)

Load (kN)

20 C, sws connection (45mm) 20D45sws

0

5

10

15

20

25

0

50

100

150

200

250

300

350

400

450

Time (mins)

Load (kN)-displacement (mm)

load

displacement

Ambiant test, swsconnection 63 mm, 20Dsws6

-5

0

5

10

15

20

25

30

35

40

45

50

0.00

1.00

2.00

3.00

4.00

5.00

6.00

7.00

8.00

time

load (kN)-displacement (mm)

Load

displacement

Ambiant test, sws connection 63mm, 20dsws7

0

5

10

15

20

25

30

35

40

0

2

4

6

8

10

12

14

Displacement (mm)

Load (mm)

Series1

Ambiant test, sws connection, 20Dsws7

0

5

10

15

20

25

30

35

40

0

50

100

150

200

250

300

350

400

time

load (kN)-displacement (mm)

load

displacement

Ambiant test, sws connection, 20dsws8

0

5

10

15

20

25

30

35

0

5

10

15

20

25

Deformation (mm)

Load (kN)

Series1

Ambiant test, sws connection, 20dsws8

-5

0

5

10

15

20

25

30

35

0

100

200

300

400

500

600

time

load (kN)-displacement (mm)

load

displacement

load-deformation, ambiant test, sws connection 45mm, 20sws452

0

5

10

15

20

25

30

0

5

10

15

20

25

30

deformation (mm)

load (kN)

load-deformation

ambiant test, sws connection 45mm, 20sws452

0

5

10

15

20

25

30

0

100

200

300

400

500

600

time (s)

load (kN)-dispalcement (mm)

load

displacement

load - deformation, ambiant test, sws connection, 63mm, 20sws453

0

5

10

15

20

25

0

5

10

15

20

25

30

35

deformation (mm)

load (kN)

load - deformation

Ambiant test, sws connection 45mm, 20sws453

0

5

10

15

20

25

30

35

00:00.0

01:26.4

02:52.8

04:19.2

05:45.6

07:12.0

08:38.4

time (s)

load (kN) - displacement (mm)

load

displacement

load-deformation, 100C heating test, sws connection 45m, 100sws45

-2

0

2

4

6

8

10

12

14

16

18

0

5

10

15

20

25

30

35

deformation (mm)

load (kN)

load-deformation

100 C heating test, sws connection 45mm, 100sws45

0

5

10

15

20

25

30

35

time

time (s)

load (kN) - deformation (mm)

deformation

load

100 C heating test, 100sws45, temperatures

0

10

20

30

40

50

60

70

80

90

100

0

1000

2000

3000

4000

5000

6000

7000

8000

9000

time (s)

temperature (C)

bolt head 1

steel plate 1

bolt 1

bolt head 2

steel plate 2

bolt 2

air temperature

100 C heating test, 100sws45, temperatures

0

10

20

30

40

50

60

70

80

90

100

0

1000

2000

3000

4000

5000

6000

7000

8000

9000

time (s)

temperature (C)

wood 1

wood 2

wood 3

wood 4

wood 5

wood 6

wood 7

load -deformation

-2

0

2

4

6

8

10

12

14

16

18

20

0

5

10

15

20

25

30

deformation (mm)

load (kN)

load -deformation

150 heating test, 150ssws1b

0

20

40

60

80

100

120

140

160

180

0

2000

4000

6000

8000

10000

12000

time (s)

temperature (C)

air temperature

bolt head 1

steel plate 1

bolt 1

bolt head 2

steel plate 2

bolt 2

150 C heating test 150ssws1b

0

20

40

60

80

100

120

0

2000

4000

6000

8000

10000

12000

time (s)

temperature (C)

wood 1

wood 2

wood 3

wood 4

wood 5

wood 6

wood 7

diagram load-deformation

0

5

10

15

20

25

30

0

5

10

15

20

25

30

35

deformation (mm)

load (kN)

Series1

Load - displacement- 200ssws5

0

5

10

15

20

25

30

35

8050

8100

8150

8200

8250

8300

8350

8400

8450

8500

8550

time (s)

load (kN) - displacement (mm)

load

displacement

200 C heating test, 200ssws5

0

20

40

60

80

100

120

140

160

180

200

0

1000

2000

3000

4000

5000

6000

7000

8000

9000

time (s)

temperature (C)

wood 1

wood 2

wood 3

wood 4

wood 5

wood 6

wood 7

load - deformation, 200 C heating test, 200sws45

0

2

4

6

8

10

12

14

16

0

5

10

15

20

25

deformation (mm)

load (kN)

load - deformation

200 C heating test, 200sws45

0

20

40

60

80

100

120

140

160

180

200

0

1000

2000

3000

4000

5000

6000

7000

8000

9000

time (s)

temperature (C)

bolt head 1

steel plate 1

bolt 1

bolt head 2

steel plate 2

bolt 2

air temperature

200 C heating test, 200sws45

0

20

40

60

80

100

120

140

160

180

0

1000

2000

3000

4000

5000

6000

7000

8000

9000

time (s)

temperature (C)

wood 1

wood 2

wood 3

wood 4

wood 5

wood 6

wood 7

280 C heating test, 280sws3

0

50

100

150

200

250

300

350

0

2000

4000

6000

8000

10000

12000

14000

time (s)

temperature (mm)

bolt head 1

steel plate 1

bolt 1

bolt head 2

steel plate 2

bolt 2

air temperature

load-deformation, 280 C heating test, 45mm, 280ssws4

0

1

2

3

4

5

6

7

8

9

0

5

10

15

20

25

30

35

deformation (mm)

load (kN)

load-deformation

280 heating test, 45mm thickness, 280ssws4

0

5

10

15

20

25

30

35

7150

7200

7250

7300

7350

7400

7450

7500

7550

7600

7650

time (s)

temperature (C)

load

deformation

280 C heating test, 45 mm thickness, 280ssws4

0

50

100

150

200

250

300

350

0

1000

2000

3000

4000

5000

6000

7000

8000

time (s)

temperature (mm)

bolt head 1

steel plate 1

bolt 1

bolt head 2

steel plate 2

bolt 2

air temperature

280 C heating test, 45 mm thickness, 280ssws4

0

50

100

150

200

250

0

1000

2000

3000

4000

5000

6000

7000

8000

time (s)

temperature (C)

wood 1

wood 2

wood 3

wood 4

wood 5

wood 6

wood 7

200

100

0

750ssws4 (sws connection, fire test)

wood 7

wood 6

wood 5

wood 4

wood 3

wood 2

wood 1

temperature (C)

time(s)

800

700

600

500

400

300

200

100

0

250

200

150

100

50

0

750ssws4 (sws connection, fire test)

300

400

500

600

700

800

0

100

200

300

400

500

600

700

800

time (s)

temperature (C)

bolt head 1

steel plate 1

bolt 1

bolt head 2

steel plate

bolt 2

air temperature

750ssws4

0

5

10

15

20

25

30

35

40

0

100

200

300

400

500

600

700

800

time(s)

load (kN) - deformation (mm)

deformation

load

750ssws5

0

100

200

300

400

500

600

700

800

0

1

2

3

4

5

6

7

8

9

10

11

Time (mins)

Load (kN)

air

wood

wood 1

wood 2

wood 3

wood 4

wood 5

wood 6

fire test, sws connection, 750ssws5

0

100

200

300

400

500

600

700

800

0.00

2.00

4.00

6.00

8.00

10.00

12.00

14.00

16.00

time (mins)

temperature (C)

bolt head 1

steel plate 1

bolt 1

bolt head 2

steel plate 2

bolt 2

750ssws5

0

1

2

3

4

5

6

7

8

9

0

2

4

6

8

10

12

14

16

Time (mins)

Load (kN)

0

5

10

15

20

25

30

35

40

45

load

deformation

750ssws6

0

100

200

300

400

500

600

700

800

0

2

4

6

8

10

12

Time (mins)

Temperature (oC)

air

wood

wood 1

wood 2

wood 3

wood 4

wood 5

wood 6

fire test, sws connection, 750ssws6

0

100

200

300

400

500

600

700

800

0.00

2.00

4.00

6.00

8.00

10.00

12.00

time (mins)

temperature (C)

bolt head 1

steel plate 1

bolt 1

bolt head 2

steel plate 2

bolt 2

750ssws6

0

1

2

3

4

5

6

7

8

9

0

2

4

6

8

10

12

Time (mins)

Load (kN)

0

5

10

15

20

25

30

35

40

45

Load

Deflection

750msws

0

5

10

15

20

25

30

0

5

10

15

20

25

30

35

40

Deformation (mm)

Load (kN)

Load

750msws

0

100

200

300

400

500

600

700

800

0

2

4

6

8

10

12

Time (mins)

Temperature (oC)

air

interface

bolt head

bolt centre

wood 1

wood 2

wood 3

wood 4

wood 5

wood 6

750msws

0

5

10

15

20

25

30

35

40

0

2

4

6

8

10

12

Time (mins)

Load (kN)

0

5

10

15

20

25

30

35

40

Load

Deformation

750swsw

0

5

10

15

20

25

30

00:00.0

02:52.8

05:45.6

08:38.4

11:31.2

14:24.0

17:16.8

20:09.6

23:02.4

time (s)

load (kN) - deformation (mm)

deformation

load

750swsw

0

100

200

300

400

500

600

700

800

00:00.0

02:52.8

05:45.6

08:38.4

11:31.2

14:24.0

17:16.8

20:09.6

23:02.4

time (s)

temperature (C)

bolt head 1

between members 1

bolt 1

bolt head 2

between timber members 2

air temperature

750swsw

-800

-600

-400

-200

0

200

400

600

00:00.0

02:52.8

05:45.6

08:38.4

11:31.2

14:24.0

17:16.8

20:09.6

23:02.4

time (s)

temperature (C)

wood 1

wood 2

wood 3

wood 4

wood 5

wood 6

750swsw2

0

5

10

15

20

25

30

35

00:00.0

02:52.8

05:45.6

08:38.4

11:31.2

14:24.0

17:16.8

20:09.6

23:02.4

time (s)

load (kN) - deformation (mm)

deformation

load

750swsw2 (fire test, wsw connection)

0

100

200

300

400

500

600

700

800

00:00.0

02:52.8

05:45.6

08:38.4

11:31.2

14:24.0

17:16.8

20:09.6

23:02.4

time(s)

temperature (C)

air

bolt head 1

between members 1

bolt 1

bolt head 2

between members 2

bolt 2

750swsw2 (fire test, wsw connection)

-100

0

100

200

300

400

500

600

700

800

00:00.0

02:52.8

05:45.6

08:38.4

11:31.2

14:24.0

17:16.8

20:09.6

23:02.4

time(s)

temperature (C)

wood1

wood 3

wood 2

wood 4

wood 5

wood 6

wood 7

Fire test, wsw connection, 750mwsw2

0

5

10

15

20

25

30

35

0

200

400

600

800

1000

1200

time (s)

temperature (C)

displacement

load

Fire test, wsw connection, 750mwsw2

0

100

200

300

400

500

600

700

800

1

36

71

106

141

176

211

246

281

316

351

386

421

456

491

526

561

596

631

666

701

736

771

806

841

876

911

946

time (s)

temperature (C)

bolt head 1

interface 1

bolt 1

bolt head 2

interface 2

bolt 2

air temperature

Fire test, wsw connection, 750mwsw2

0

100

200

300

400

500

600

1

33

65

97

129

161

193

225

257

289

321

353

385

417

449

481

513

545

577

609

641

673

705

737

769

801

833

865

897

929

time (s)

temperature (C)

wood 1

wood 2

wood 3

wood 4

wood 5

wood 6

wood 7

fire test, wsw connection, 750mwsw3

0

5

10

15

20

25

30

35

0

200

400

600

800

1000

1200

time (s)

temperature (C)

displacement

load

Fire test, wsw connection, 750mwsw3

0

100

200

300

400

500

600

700

800

1

35

69

103

137

171

205

239

273

307

341

375

409

443

477

511

545

579

613

647

681

715

749

783

817

851

885

919

time (s)

temperature (C)

bolt head 1

interface 1

bolt 1

head bolt 2

interface 2

bolt

air temperature

Fire test, wsw connection, 750mwsw3

0

50

100

150

200

250

300

1

32

63

94

125

156

187

218

249

280

311

342

373

404

435

466

497

528

559

590

621

652

683

714

745

776

807

838

869

900

time (s)

temperature (C)

wood 1

wood 2

wood 3

wood 4

wood 5

wood 6

wood 7

750swww (fire test, www connection, one bolt)

0

100

200

300

400

500

600

700

800

0

200

400

600

800

1000

1200

1400

time (s)

temperature (C)

wood 1

wood 2

wood 3

bolt in the side member 1

bolt in the side member 2

wood in the side member 1

wood in the side member 2

750swww (fire test, www connection, one bolt)

0

100

200

300

400

500

600

700

800

0

200

400

600

800

1000

1200

1400

time (s)

temperature (C)

air

bolt head 1

between timber members 1

bolt 1

bolt head 2

between timber members 2

bolt 2

750swww (fire test, www connection)

0

5

10

15

20

25

30

35

40

0

200

400

600

800

1000

1200

1400

time (s)

load (kN) - displacement (mm)

displacement

load

750swww2 (fire test, www connection)

0

100

200

300

400

500

600

700

0

200

400

600

800

1000

1200

1400

time (s)

temperature (C)

wood 1

wood 2

wood 3

bolt in side member 1

bolt in side member 2

wood side member 1

wood side member 2

750swww2 (fire test, www connection)

0

200

400

600

800

1000

1200

0

200

400

600

800

1000

1200

1400

time (s)

temperature (C)

bolt head 1

between timber members 1

bolt 1

bolt head 2

between timber members 2

bolt 2

air temperature

fire test, www connection, 750swww2

0

5

10

15

20

25

30

35

40

0

200

400

600

800

1000

1200

1400

time (s)

load (kN) - displacement (mm)

displacement

load

Fire test, www connection, 750mwww

0

5

10

15

20

25

30

35

40

1

13

25

37

49

61

73

85

97

109

121

133

145

157

169

181

193

205

217

229

241

253

265

277

289

301

313

325

337

time (s)

load (kN) - deformation (mm)

deformation

load

Fire test, www connection, 750mwww

0

100

200

300

400

500

600

700

800

900

0

200

400

600

800

1000

1200

1400

1600

time (s)

temperature (C)

bolt head 1

between two members 1

bolt 1

bolt head 2

between two members 2

bolt 2

air temperature

fire test, www connection, 750mwww

0

100

200

300

400

500

600

700

0

200

400

600

800

1000

1200

1400

1600

time(s)

temperature (C)

wood middle member 1

wood middle member 2

wood middle member 3

bolt side member 1

bolt side member 2

wood side member 1

wood side member 2

fire test, www connection, 750mwww2

0

5

10

15

20

25

30

35

0

200

400

600

800

1000

1200

1400

time (s)

load (kN) - deformation (mm)

deformation

load

fire test, www connection, 750mwww2

0

100

200

300

400

500

600

700

800

900

0

200

400

600

800

1000

1200

1400

time (s)

temperature (C)

bolt head

between timber members

bolt

bolt head 2

between timber members2

bolt 2

air temperature

fire test, www connection, 750mwww2

0

100

200

300

400

500

600

0

200

400

600

800

1000

1200

1400

time (s)

temperature (C)

wood middle member 1

wood middle member 2

wood middle member 3

bolt side member 1

bolt side member 2

wood side member 1

wood side member

prediction of fire resistance using johansen's equations for the test 750ssws6

-10

0

10

20

30

40

50

60

0

100

200

300

400

500

600

700

time (s)

failure load (kN)

deformation

mode k

mode j or l

mode m

applied load

fire resistance prediction using johansen's equations for the test 750ssws5

-10

0

10

20

30

40

50

60

0

100

200

300

400

500

600

700

800

900

1000

time (s)

failure load (kN)

deformation

mode k

mode j or l

mode m

load applied

Prediction of the failure load for the test 750ssws4

-10

0

10

20

30

40

50

60

0

100

200

300

400

500

600

700

800

time

failure load (kN)

-deformation (mm)

deformation

mode k

mode j or l

mode m

load applied

experimental

failure

prediction of the fire resistance of the 750msws3 test, using johansen's equations

0

50

100

150

200

250

0

100

200

300

400

500

600

700

800

time (s)

failure load (kN)

displacement

mode k

mode j or l

mode m

load applied

prediction of the fire resistance for the 750msws2 test, using Johansen's equations

0

50

100

150

200

250

0

100

200

300

400

500

600

700

800

time (s)

failure load (kN)

displacement

mode k

mode j or l

mode m

load applied

prediction of the fire resistance for the test 750msws1, using Johansen's equations

0

50

100

150

200

250

0

100

200

300

400

500

600

700

800

time (s)

failure load (kN)

displacement

mode k

mode j or l

mode m

load applied

prediction of the time to failure for the test 750mwsw3

-50

0

50

100

150

200

250

0

200

400

600

800

1000

1200

time (s)

failure load (kN)

mode f

mode g

mode h

load applied

displacement

prediction of the time to failure of the test750mwsw2 using Johansen's equation

0

50

100

150

200

250

0

200

400

600

800

1000

1200

time (s)

failure load (kN)

mode f

mode g

mode h

applied load

Series5

prediction of the fire resistance of the 750swsw2 test, using johansen's equations

0

10

20

30

40

50

60

0

200

400

600

800

1000

1200

1400

time (s)

failure load (kN)

displacement

mode f

mode g

mode h

load applied

prediction of the fire resistance of the test 750mwww1, using johansen's equations

-50

0

50

100

150

200

250

300

0

200

400

600

800

1000

1200

1400

1600

time (s)

failure load (kN)

deformation

mode g

mode h

mode j

mode k

load applied

prediction of the fire resistance using johansen's equation for the test 750swww2

0

10

20

30

40

50

60

0

200

400

600

800

1000

1200

1400

time (s)

failure load (kN)

displacement

mode g

mode h

mode j

mode k

load applied

prediction of the failure load of the test 750swww

-10

0

10

20

30

40

50

60

0

200

400

600

800

1000

1200

1400

time (s)

failure load (kN)

deformation

mode g

mode h

mode j

mode k

load applied

experimental

failure

prediction of the failure for the test 750mwww2, using johansen's equations

0

50

100

150

200

250

300

0

200

400

600

800

1000

1200

1400

time (s)

failure load (kN)

displacement

mode g

mode h

mode j

mode k

load applied

750msws3

0

5

10

15

20

25

30

35

0

100

200

300

400

500

600

700

800

time (s)

Load  (kN)- displacement (mm)

displacement

load

750msws3

0

100

200

300

400

500

600

700

800

0

100

200

300

400

500

600

700

800

time(s)

temperature (C)

air

bolt head average

steel plate average

bolt average

wood average

750msws2

0

5

10

15

20

25

30

35

40

0

100

200

300

400

500

600

700

800

time(s)

load (kN) - displacement (kN)

displacement

load

750msws2

0

100

200

300

400

500

600

700

800

0

100

200

300

400

500

600

700

800

time (s)

temperature (C)

bolt head (average)

steel plate average

bolt average

wood average

air

temperature in the timber

0

50

100

150

200

250

300

350

400

0

100

200

300

400

500

600

700

Time (s)

Temperature (C)

timber (32 mm

depth)

timber (22 mm)

timber (12 mm)

timber (7 mm)

timber (2 mm)

experimental-

timber (32mm)

temperature in the bolt in a sws connectrion during a fire test

0

50

100

150

200

250

300

350

400

450

500

0

100

200

300

400

500

600

700

800

900

Time (s)

Temperature (C)

numerical-bolt

numerical-timber

(1mm from bolt)

numerical-

timber(2mm from

bolt)

experimental-bolt

mode k

Failure load (kN)

time (s)

900

800

700

600

500

400

300

200

100

0

60

50

40

30

20

10

0

prediction of the fire resistance of a sws connection with one bolt using safir

mode j or l

mode m

load applied

Prediction of the failure load of a sws connection with 4 bolts using the results of safir in

Johansen's equation

0

50

100

150

200

250

0

100

200

300

400

500

600

700

800

900

time (s)

load (kN)

mode k

mode j or l

mode m

load applied

temperature in the timber in a wsw connection at different depth during a fire

-100

0

100

200

300

400

500

600

700

800

0

200

400

600

800

1000

1200

Time (s)

Temperature (C)

timber exterior

timber (9mm depth)

timber (18mm depth)

timber (27 mm depth)

timber (36mm depth)

interface timber-steel plate (45

mm depth)

temperature in a bolt and in the timber around in a wsw connection during a fire

0

100

200

300

400

500

600

700

0

200

400

600

800

1000

1200

Time (s)

Temperature (C)

bolt

timber (2mm from bolt)

timber (4mm from bolt)

timber (6mm from bolt)

bolt head

interface bolt-steel plate

prediction of the fire resistance of a wsw connection with one bolt using safir

0

10

20

30

40

50

60

0

200

400

600

800

1000

1200

Time (s)

Temperature (C)

mode f

mode g

mode h

load applied

prediction of the failure load of a wsw connection with 4 bolts using safir

0

50

100

150

200

250

0

200

400

600

800

1000

1200

time (s)

load (kN)

Series1

Series2

Series3

Series4

temperature in the bolt

0

100

200

300

400

500

600

700

0

200

400

600

800

1000

1200

1400

Time (s)

Temperature (C)

swww1 test

swww2 test

numerical results

temperature in the bolt and in the timber around in a www connection during a fire

0

50

100

150

200

250

300

350

400

0

200

400

600

800

1000

1200

Time (s)

Temperature (C)

bolt

timer (3mm from bolt)

timber (6mm from bolt)

timber (9mm from bolt)

Temperature in the timber of a www connection for diffetent depth during a fire

-100

0

100

200

300

400

500

600

700

800

0

200

400

600

800

1000

1200

Time (s)

Temperature (C)

Series1

Series2

Series3

Series4

Series5

Series6

Series7

Series8

Series9

Series10

Series11

Series12

Series13

temperature in the timber in a www connection during a fire

-50

0

50

100

150

200

250

300

350

400

450

500

0

200

400

600

800

1000

1200

1400

Time (s)

Temperature (C)

timber (middle member)

timber (side member)

numerical result (middle member)

2

numerical result (middle member)

prediction of the time to failure of a www connection with one bolt during a fire using safir

0

10

20

30

40

50

60

0

200

400

600

800

1000

1200

time (s)

load (kN)

mode g

mode h

mode j

mode k

load applied

prediction of the failure load of a www connection with 5 bolts using safir

0

50

100

150

200

250

300

0

200

400

600

800

1000

1200

time (s)

load (kN)

Series1

Series2

Series3

Series4

Series5